## Slide 1: Mechanical Characterization of Nano-scale Interfaces in Biocomposite Material
Mohammad Tadayon B CUBE – Center for Molecular Bioengineering, Technical University of Dresden, Germany
TAC Meeting 10.02.2021

## Slide 2
OUTLINE
Introduction
- Biological materials and their mechanical properties
- Interfaces in biocomposite material
Purpose of the study
- Challenges
Three main approaches to conduct the study
- Theoretical
- Instrumental
- Experimental
Work Plan

## Slide 3
MECHANICAL PROPERTIES OF BIOMATERIALS
Complex composite materials with diverse mechanical functionalities
Properties are achieved through hierarchical structuring over many length scales
U. Wegst et. al. , Nature Materials, 2014

## Slide 4
HIERARCHY
Nacre
Bone
U. Wegst et. al. , Nature Materials, 2014

## Slide 5
INTERFACES IN BIOCOMPOSITE
Mineral
– Stiffness
– Strength
Organic Interfaces
– Toughness
– Deformability
– Viscoelasticity
Dunlop et al., MATERIALS TODAY (2011)
Interfaces Improving
Material Toughness
Interfaces Allowing
Materials to Deform
Interfaces Allowing
Materials to Move
Interfaces Bridging
Different Materials
~ 1 µm ~ 40 nm ~ few nm
Tough, stiff and stable bodies with the capability to creep, recover, undergo stress relaxation, absorb energy and more…
Coccolithophore
Pinna Nobilis
Perna Canaliculus

## Slide 6
CHALLENGES
Environmental Dependence
Interfaces are Small
How to Probe Dynamic and Static Performance of a Single Interface – Elasticity, Plasticity and Viscoelasticity?
~ 1 µm
~ 40 nm
~ few nm
B. Bayerlein et. al. , Advanced Functional Materials, 2016
H. M. Drezner et. al. , Advanced Functional Materials, 2010
Peisker et al., Nat. Commun. , 2013
Coccolithophore
Pinna Nobilis
Perna Canaliculus
Pine Cone
Seed Capsule

## Slide 7
PURPOSE OF PhD STUDY
A multi-disciplinary and collaborative study
Mechanical Characterization of Nano-scale Interfaces in Biocomposite Material
Objectives:
To develop and test Theoretical/Instrumental/Experimental frameworks to probe the mechanical properties of mineral/organic interfaces in biocomposites as a function frequency and environmental properties.
Zlotnikov’s Lab.
Bar-On’s Lab. (Ben-Gurion University)

## Slide 8
NANOINDENTATION BASED METHODS
Three main approaches
Theoretical
Instrumental
Experimental

## Slide 9
THEORETICAL

## Slide 10
Nano-SCALE MODULUS MAPPING
Nanoscale Dynamic Mechanical Analysis
Cupiennius salei Cuticle (Tibia):
3x3 µm
Anchor spicule in Monorhaphis chuni:
5 µm
Scanning Probe Microscopy (SPM)
I. Zlotnikov et. al. , Progress in Materials Science , 2017

## Slide 11
THEORETICAL
We defined a fully analytical description for a contact problem across an interface.
Developing a method for Modulus Mapping to formulate contact with an interface boundary
K. Tadayon et. al. , Extreme Mechanics Letters, 2021
Notes: Therfore we need to understand better the effect of distance from the interface, so we reploted all the data in another format, force vs. distance from the interface at 6 different depth of penetration. As can be seen in this diagram, far from the interface we have plateus. Obviously, the left ones correspond to the indents on silica and right ones correspond to the indents on Si.
But in between we have an assymetric growth, therefore we proposed an unlinear weight function. A sigmoidal function which is able to weigh the force close to the interface.
Now we need to find the parameters b and a. Using the boundary condition at the interface from the previous slide, we conclude that b=2 and therefore this formula.
Interestingly, the formula fits perfectly to all the curves. After fitting we measured the parameter a at each displacement which are ploted on the right hand-side figure. This prameter is beautifully fitted with the radius of the contact area.
Therefore we could physically defined an analytical description for a contact problem across an interface.

## Slide 12
FINITE ELEMENT MODELING
By fitting
By fitting
The FEM data validates the hypothesis well.
Sneddon Model
Hertz Model
K. Tadayon et. al. , Extreme Mechanics Letters, 2021
Notes: We plotted the FEM data, and as you can see the analytical description fits very well to not only the data from Hertz model but also Sneddon model.
There is only, a small difference.
As for sneddon model, we have a flat-ended cylinder and at different depth of penetration the contact area is constant and the radius of the contact area is exactly the radius of our cylinder.

## Slide 13
Nano-SCALE MODULUS MAPPING
The formula well-predicts the effective elastic modulus and it can be a stepping-stone toward establishing an analytical expression for contact with multilayered biocomposite architectures.
Scan size: 2.52.5 µm2
Contact force: 200 µN
Dynamic force: 20 µN
Frequency : 205 Hz
K. Tadayon et. al. , Extreme Mechanics Letters, 2021
Notes: The last but not the least, we investigated if we can predict effective elastic modulus at different distances from the interface while doing modulus mapping.
Based on the developed descriction, we derived the formula on the top right side which is the effectic elastic modulus as a function of distance from interfce. With this we could well predict the modulus mapping data which are mesured from the shaded rectangular area.

## Slide 14
INSTRUMENTAL

## Slide 15
ENVIRONMENTAL CONTROL
High Temperature Stage with Inert Gas Infrastructure (xSol)
Humidity Generator
Humidity Temperature Sensor
THE SET-UP:
L. Bertinetti et. al. , Philosophical Magazine, 2015
Our In-house Set-up
Can we also observe the sample while indenting and controlling the humidity ?

## Slide 16
INSTRUMENTAL
Environmental Control
Developing a setup for a picoindenter inside an environmental SEM to do in-situ indentation while controlling the humidity and temperature!
Notes: Contact mechanics is a study of deformation of bodies which are in contact with one or more points.
It has lots of engineering and scientific applications such as locomotive rail wheel contact, the design of hip joints, the principles of atomic force microscopy and so on.
The contact can be elastic, viscoelestic or plastic. But today I am going to focus only on elastic contact mechanics.
Two of the most commonly used theories in elastic contact mechanics are ...

## Slide 17
EXPERIMENTAL

## Slide 18
EXPERIMENTAL
Model System
Calcite/Organic prismatic structure in mollusks (A. vexillum)
Amorphous Silica/Organic periodic structure in the spicules of marine sponges (M. chuni)
Experiments:
1- Direct approach
2- Indirect approach
I. Zlotnikov et. al. , RSC Advances, 2013
D. Zöllner et. Al. ,Materials Horizons, 2019
Notes: Contact mechanics is a study of deformation of bodies which are in contact with one or more points.
It has lots of engineering and scientific applications such as locomotive rail wheel contact, the design of hip joints, the principles of atomic force microscopy and so on.
The contact can be elastic, viscoelestic or plastic. But today I am going to focus only on elastic contact mechanics.
Two of the most commonly used theories in elastic contact mechanics are ...

## Slide 19
PROBING A SINGLE INTERFACE
To study the behavior of a single interface decoupled from the geometry of the composite
To measure its elastic, plastic and viscoelastic response
B. Bar-On et. al. , Physical review letters, 2017

## Slide 20
EXPERIMENTS
Relaxation analysis
(micro-pillar compression)
Bending analysis
(micro-cantilevers vibrations)
Torsion analysis
(micro-key vibrations)
Notes: Contact mechanics is a study of deformation of bodies which are in contact with one or more points.
It has lots of engineering and scientific applications such as locomotive rail wheel contact, the design of hip joints, the principles of atomic force microscopy and so on.
The contact can be elastic, viscoelestic or plastic. But today I am going to focus only on elastic contact mechanics.
Two of the most commonly used theories in elastic contact mechanics are ...

## Slide 21
MICRO-CANTILEVERS VIBRATIONS
Notes: Contact mechanics is a study of deformation of bodies which are in contact with one or more points.
It has lots of engineering and scientific applications such as locomotive rail wheel contact, the design of hip joints, the principles of atomic force microscopy and so on.
The contact can be elastic, viscoelestic or plastic. But today I am going to focus only on elastic contact mechanics.
Two of the most commonly used theories in elastic contact mechanics are ...

## Slide 22
WORK PLAN
Work Packages | Feb. – May. | Jun. – Sep. | Oct. – Jan. | Feb. – Jul.
FIB-SEM sample preparation |  |  |  | 
Instrumental project |  |  |  | 
Direct measurements (nanoDMA and modulus mapping) |  |  |  | 
Indirect measurements (bending and shearing experiments) |  |  |  | 
Writing thesis |  |  |  | 
Overview of the time schedule for the continuation of the study in 2022 and 2023:

## Slide 23
Acknowledgements
  Dr. Igor Zlotnikov
  Prof. Benny Bar-On
  Dr. Robert Lemanis
  Dr. Elke Reich
  Zlotnikov‘s Group
Thank you for your attention!