## Slide 1: Sliding contacts in liquid environments: Nanotribology in Liquid
Thesis Advisory Committee
Progress Report
Dennis Kang
Jan 2023

## Slide 2
Agenda
Brief background
  Friction Force Microscopy in liquid
  Prandtl-Tomlinson model
  Piezo-electric sensors
  Normal & Lateral Force calibrations
Results and Potential publications
  Tribolayer phenomenon of MoS2 in PYR-14 TFSI ionic liquid
  Milestone
What needs to be done in the future
Questions to consider
Jan 2023

## Slide 3
Laser is directed onto the back coating of the cantilever then reflected towards the photodetector
Photodetector experiences an exaggerated movement of the laser position
  Topography (height) is recorded along the scan direction
Torsion bending of the cantilever is also recorded
  Torsion angle is proportional to the friction / lateral force (↗ Torsion = ↗ Friction)
Software projects these signals into an image (line by line)
Friction Force Microscopy
[1] https://nunano.com
[2] https://www.ntmdt-si.com/resources/spm-principles/atomic-force-microscopy/contact-afm
Jan 2023
[1]
[2]

## Slide 4
Friction Force Microscopy in liquid
Probe holder = Glass block
  Transparency allows laser to go through
Meniscus formation
  Liquid droplets are squeezed in between the sample and the probe holder = ↓ Friction variation (i.e. capillary condensation) = ↑ image quality
Closed-cell is no different
  Restricts liquid to escape (i.e. volatile liquids)
Mica in Water (20 x 20 nm2)
Open-cell configuration
Top
Bottom
Jan 2023

## Slide 5
Prandtl-Tomlinson (PT) model
[3]M. R. Vazirisereshk, K. Hasz, R. W. Carpick, A. Martini, J. Phys. Chem. Lett, 2020, 11, 6900-6906
[4] K. Tian, D. L. Goldsby, and R. W. Carpick, Phys. Rev. Lett, 2018, 120, 186101
[5] J. S. Helman, W. Baltensperger, and J. A. Holyst, Simple model for dry friction, Phys. Rev. B 49, 3831 (1994)
Jan 2023
[5]
Potential Energy Profiles
  Atoms are arranged
  as corrugated energy wells
Stick-Slip motion
  Tip (point-mass) is being pulled as it climbs up the energy well (atom), but slight resistance (friction) is present = Stick
  The tip attains enough energy to overcome the energy well, relaxing immediately after passing the peak = Slip
[3]
[4]
Saw tooth (stick-slip) profile of MoS2

## Slide 6
Piezo-electric scanners
[6] Multimode SPM Instruction Manual, p.23
Jan 2023
[6]
2 types, but same principle
  AFM Head (Nanowizard, Nanosurf, Bioscope)
  Sample base (Multimode)
Voltage application
  Planar XY raster pattern
  ↓ Scanner Size = ↓ Acoustic noise = ↑ Precision (i.e. atomic scale)
A | E | J
Superior atomic resolution (size range 8 - 400 nm2) | Mid-range between A and J (max. size up to 10 μm2) | Auto tripod adjustment (max. size up to 125 μm2)
Manual tripod adjustment is required, Poor Z-position stability (E - piezo is more stable) |  | Cannot attain atomic resolution
slow (Y) axis
Fast (X) axis
J - piezo
A - piezo
Tripod adjustment nozzles

## Slide 7
Force calibrations
All corresponding forces are measured in Voltages
Normal Force (FN)
  Force-Distance curve
  Thermal oscillation method (not available in Multimode AFM)
Friction Force (FF)
  TGG1 calibration gratings
    Varying normal force to identify conversion ratio between V and nN
  Conversion formulae
    Fast estimation
    incompatible with thermal oscillation method
[7] https://www.ntmdt-tips.com/products/view/tgg1
Jan 2023
Gradient
= Sensitivity (S)
Adhesion
[7]

## Slide 8
Results and potential publications
Jan 2023
In Progress…
  MoS2 in PYR-14 TFSI ionic liquid
    Friction transition of tribolayer penetration
Pending
  Single Material, Several liquids
    MoS2 in air (reference), water, PYR-14 TFSI, BMIM-PF6
  Several Materials, Single liquid
    Mica, NaCl, CaCO3, MoS2, in BMIM-PF6

## Slide 9
10 x 10 nm2 | Pre-transition |  |  | 
Set-Point (nN) | iGain (Hz) | 50 | Line Rate (Hz) | 50
98 | PGain | 0.001 | Tip Velocity (μm∙s-1) | 1.56
10 x 10 nm2 | Moment of transition |  |  | 
Set-Point (nN) | iGain (Hz) | 50 | Line Rate (Hz) | 50
98.5 | PGain | 0.001 | Tip Velocity (μm∙s-1) | 1.56
10 x 10 nm2 | Post-transition |  |  | 
Set-Point (nN) | iGain (Hz) | 50 | Line Rate (Hz) | 50
103 (max.) | PGain | 0.001 | Tip Velocity (μm∙s-1) | 1.56
Sample | Medium / Mode | Image (Pixels) | Cantilever | Measurement Date
MoS2 (Bulk_sheet) | PYR14 - TFSI / Contact Mode | Lateral Deflection (512 x 512) | SNL-10_D (no.10) | 24 – JUNE – 2021

## Slide 10
Sample | Medium / Mode | Graph | Cantilever | Measurement Date
MoS2 (Bulk_sheet) | PYR14 - TFSI / Contact Mode | Set-point vs Mean Lateral Deflection | SNL-10_D (no.10) | 25 – JUNE – 2021
Pre-Transition (FN = 88.5 nN)
Post-Transition (FN = 92.5 nN)
Bulk MoS2 in PYR14-TFSI
Friction (uncalibrated) vs normal force plots of MoS2 in PYR14-TFSI IL
Jan 2023
Notes: 10

## Slide 11
MoS2 in PYR-14TFSI
[8] R.An et al. Nanoscale, 2022, 14, 11098-11128
Jan 2023
‘’Atomic force microscopy probing interactions and microstructures of ionic liquids at solid surfaces’’ by Rong An et al.
  Load dependence relationship of the graphite (HOPG) and mica in ionic liquid
    Same ionic liquid (MBIM-PF6) was used in this publication
  Instead of sharp tip, they used colloidal silica probe (more common in this field)
    their lattice scale image is missing
There is a chance to establish tribolayer related phenomenon with comparable dataset beyond state of the art
[8]

## Slide 12
Milestone
Jan 2023
 | MoS2 Bulk sheet | Mica | CaCO3 (Calcite) | NaCl (Salt crystal)
Air (Reference) | ○ (Jena 2021) | ○ (Dresden 2021) | ○ (Dresden 2021) | ○ (Dresden 2022)
Water |  | ○ (Dresden 2022) | ○ (Dresden 2022) | 
PYR-14 TFSI (Jena) | ○ (Jena 2021) | ○ (Krakow 2022) | ○ (Krakow 2022) | 
BMIM-PF6 (Israel) | ○ (Krakow 2022) | ○ (Krakow 2022) |  | 
Some of the dataset needs to be repeated with Multimode (Dresden)
  To ensure its consistency with other hardware
  i.e. Nanosurf (Krakow), Nanowizard (Jena)
  Troubles with friction force calibration
    Possible solution: Apply average of all previously measured conversion ratio

## Slide 13
What needs to be done in the future
Jan 2023
Complete rest of the dataset
  Different ionic liquids and materials
  Replication with Multimode
Explain the chemistry of tribolayer phenomenon
  Prof. Berkovich may be able to help with his background knowledge
  Simulation of PT model in liquid
Compare the dataset with the colloidal probe measurements in IL
Produce drafts for the publication