## Slide 1: Inkjet printed Gas Sensors based on 2D materials
Abdallh Herbawe
Olfactorial Perceptronics
Chair for Materials Science and Nanotechnology, TU Dresden
Thesis Advisory committee (TAC) Kick-off meeting
Friday, January 26, 2024

## Slide 2: Outline
Introduction
    2D materials
    What Are MXenes?
    Why MXenes for gas sensing?
    MXenes based gas sensors in Literature today!
    Strategies for modifying MXenes for gas sensing?
    Why Inkjet Printing?
Project goals
Project Plan
Results and proof of concepts
Research Time table
Proof of concept and results so far

## Slide 3: 2D Materials
Graphene
MXene
BP
Polymer
Metal oxides
MOFs
LDHs
TMDs
H-BN
High Surface Area
Tunable Electronic Properties
High Electron Mobility
Chemical Sensitivity
Potential for Multifunctionality

## Slide 4: Introduction: What Are MXenes?
A family of 2D materials consisting of:
Transition metal.
Carbides/nitrides/Carbonitrides/oxycarbides.
They are general made of etching away Al in MAXene precursors such as Ti2AlC, or Ti3AlC2.
MXenes are generally represented by Mn+1XnTx
M represents an early transition metal.
X denotes either carbon, nitrogen, carbonitride, or oxycarbide.
T represents surface terminations on the outer transition metal layers.
Credit: © Martin Künsting/HZB

## Slide 5: Introduction: Why MXenes for gas sensing?
High conductivity
high signal-to-noise ratio
Large surface area
POSITIVES
NEGATIVES
Cross-interference
Low band-gap
Base line drift
easily degraded in moisture environment

## Slide 6: Introduction: MXenes based gas sensors in Literature today!
M. Sai Bhargava Reddy, Coordination Chemistry Reviews (2024)

## Slide 7: Introduction: Strategies for modifying MXenes for gas sensing?
M. Sai Bhargava Reddy, Coordination Chemistry Reviews (2024)
Surface terminations
Intercalation
(inserted ions)
No terminations
Atomic
vacancy
Heteroatom
doping
Surface oxidation
Surface
functionalization

## Slide 8: Introduction: Why Inkjet Printing?
M. Sai Bhargava Reddy, Coordination Chemistry Reviews (2024)

## Slide 9: Research Goals
Fabrication of Inkjet printed 2D materials based gas sensors for smart olfactory mimicking and sensing of H2S and H2

## Slide 10: Research Plan
Mxene
Synthesis
Synthesis of Titanium Carbide Mxenes
Growing gold nano structures on Mxene sheets
Formulating ink for inkjet printing out of the Mxene sheets
Inkjet printing gas sensor with Mxene sheets as sensing material
Conducting Gas sensing experiments
Surface Modification
Ink
Formulation
Sensor Fabrication
Gas
Sensing
Other modifications

## Slide 11: Research time table
Mxene
Synthesis
Ink
Formulation
Gas
Sensing
Other modifications
Sensor Fabrication
Surface Modification
Task | 2024 1st half |  | 2024 2nd half |  | 2025 1st half |  | 2025 2nd half |  | 2026 1st half |  | 2026 2nd half | 
Synthesis of Titanium Carbide Mxenes |  |  |  |  |  |  |  |  |  |  |  | 
Growing gold nano structures on Mxene sheets |  |  |  |  |  |  |  |  |  |  |  | 
Formulating ink for inkjet printing out of the Mxene sheets |  |  |  |  |  |  |  |  |  |  |  | 
Inkjet printing gas sensor with Mxene sheets as sensing material |  |  |  |  |  |  |  |  |  |  |  | 
Conducting Gas sensing experiments |  |  |  |  |  |  |  |  |  |  |  | 
Other modifications |  |  |  |  |  |  |  |  |  |  |  | 

## Slide 12: Proof of concept and results so far
Graphene was used so far, but it proved:
    The ability to print stable and repeatable advanced nanomaterials patterns.
    The ability to control the pattern dimensions down to 11 .
Graphene and CNTs are other materials that could be also an interest in future implementations and modifications.