## Slide 1: TAC meeting
Kwan Ho Au-Yeung
Single Molecule Machines Group, cfaed, TU Dresden, Germany
17.11.2022

## Slide 2: Content
1. Transmitting rotation between molecule-gears
2. Exploring new on-surface synthesis pathway – Knoevenagel condensation
3. Molecule-rotor and nanocar – E-DMBI-P

## Slide 3: Motivation: Transmiting rotation between molecule-gears
Molecular gears
Transmission of motion
Molecular mechanical device
Information
Information

## Slide 4: Optimizing under Pentaphenylcyclopentadiene (PPCP) framework
On-surface anchoring strategy
Marker for visualization
Optimization for transmitting rotation
Tip-induced manipulation
STM Tip
Manipulation
Total: 5 designs

## Slide 5: PPCP-tert-butyl
Evaporation: T = 180 °C; t = 30 s
2.5 x 2.5 nm²/15 x 15 nm², 7.2 pA, 500 mV
Au(111)

## Slide 6: Single molecule-gear rotation
6.5 x 6.5 nm², 13 pA, 530 mV
Red arrows indicate the trajectories of lateral manipulations (V = 10 mV and I = 8 pA; Tunneling resistance = 1.25 GΩ) achieved by STM tip

## Slide 7: Two interlocked gears
6.5 x 6.5 nm², 13 pA, 530 mV
Red arrows indicate the trajectories of lateral manipulations (V = 10 mV and I = 8 pA; Tunneling resistance = 1.25 GΩ) achieved by STM tip

## Slide 8: Three interlocked gears
6.5 x 6.5 nm², 1.9 pA, 530 mV
Red arrows indicate the trajectories of lateral manipulations (V = 10 mV and I = 14 pA; Tunneling resistance = 0.71 GΩ) achieved by STM tip

## Slide 9: On-surface synthesis – examples of pathways
Chem. Rev., 119, 7, 4717-4776 (2019)
We need more!

## Slide 10: Exploring new on-surface synthesis pathway
Precursor 4-formyl(4,4’’-terphenyl)-4’’-methylenenitrile
Intermediate
Final Conjugated oligo-phenylenevinylenes (PV)
Goal:
On-surface reactions between aldehydes and methylene nitriles
 CN-substituted structures coupling with C=C bond
STM tip
STM imaging at 5K

## Slide 11: Stepwise post-annealing on Au(111)
Anneal @200°C
Anneal @220°C
Anneal @240°C
Deposition @RT
(23 nm x 23 nm); V = 300-500 mV and I = 3-10 pA
Monolayer islands
Diffusion and desorption
Reaction and desorption
Further desorption

## Slide 12: Knoevenagel condensation activated on Au(111)
(4.6 nm x 1.1 nm); V = 10 mV
Constant height CO-tip
Calculated adsorption geometry
Calculated trimer structure
Calculations from Dmitry A. Ryndyk

## Slide 13: Single-molecule machines Movement induced by inelastic electron tunneling
Motion activated by voltage pulses with the STM tip
Energy is introduced by inelastic tunneling
Most of the tunneling current is however elastic
Electric field always present between STM tip and surface
V, I
t
A.M. Moore and P.S. Weiss, Annu. Rev. Anal. Chem. 1, 857 (2008)
V, I, t

## Slide 14: Single-molecule rotor (Previous results) Chemically anchored DMBI-P
Anchoring reaction
heating in UHV
o-MeO‑DMBI‑I
molecule-rotor
DMBI‑P
chemisorption
-MeI
on Au(111)
F. Eisenhut, et al. Nanoscale 13, 16077 (2021)
DMBI-P: 2-(1,3-dimethyl-1H-benzo[d]imidazol-3-ium-2-yl)-phenolate
Notes: Iodine dissociation, resulting in a radical form. Alternative: cleavage of the O–Me bond and the elimination of methyl iodide (MeI). Not a radical

## Slide 15: Single-molecule rotor Adding a ring – Extended DMBI
Single molecules (low coverage)
Same behavior as DMBI-P by voltage pulses (typically V = 500 mV, I = 500 pA)
Unidirectional rotation
A left-DMBI-P, always rotates CCW by positive voltage pulses
x
x
x
x
x
x
I = 250 pA and V = 0.5 V

## Slide 16: From rotor to nanocar Both rotors and nanocars after dimer separation
Separated dimers form a rotor and a nanocar (60%) or two nanocars (40%)
Typical voltage pulses of V = 0.5 V and I = 500 pA move both
4 nm x 4 nm

## Slide 17: Nanocar Controlled translation by voltage pulses
Tip at a lateral distance of 1–1.5 nm (red mark), pulse V ≥ 0.4 V, I ≥ 100 pA
By positive voltage pulses, the molecule is attracted by the tip independently on its chirality (379 pulses)
By negative voltage pulses, the molecule moves less and randomly away from the tip
V > 0
V < 0

## Slide 18
Thank You!
Publications:
K.H. Au Yeung, T. Kühne, F. Eisenhut, M. Kleinwächter, Y. Gisbert, R. Robles, N. Lorente, G. Cuniberti, C. Joachim, G. Rapenne, C. Kammerer, and F. Moresco. J. Phys. Chem. Lett. 2020 11 (16), 6892-6899.
K. H. Au-Yeung, T. Kühne, D. Becker, M. Richter, D. A. Ryndyk, G. Cuniberti, T. Heine, X. Feng, F. Moresco. Chem. Eur. J. 2021, 27, 17336.
In preparation.
1)
2)
3)