## Slide 1
Yuru Ge · y.ge@hzdr.de
HZDR / TU Dresden 2nd March 2023
Time-dependency of martensitic transformation in ferromagnetic Ni-Mn-Ga-based epitaxial films
1rd TAC meeting of PhD Thesis

## Slide 2: Martensitic transformation in ferromagnetic materials
What’s the difference if we heat/cool in different time-scales ?
(from ~ns laser to ~h metal heating)
Why ?
x-variant
z-variant
y-variant
a
a
a
a
a
a
a
c
c
c
Cooling
Ferromagnetic
Low-symmetry
Martensites
Heating
Non-magnetic
High-symmetry
Austenite
Example: Ni-Mn-Ga

## Slide 3: Motivation: why study time-dependency martensitic transformation?
[1] R. Kainuma et al. Nature. 2006;439:957–960.
[2] J. Liu et al. Nat Mater. 2012;11:620–626.
[3] M. Gueltig et al.. Adv Energy Mater. 2017;7:1601879.
How?
To drive the applications faster
Transform
Switch
reversible cycles
releases heat
absorbs heat
M>>0
M=0
M>>0
M=0
Apply
Magnetic
field
remove field
…actuation[1]:
…magnetocaloric refrigeration[2]:
…energy harvesting[3]:
H
H
low temperature waste heat
Reversible, thermoelastic martensitic transformations
Switch material’s crystal system by temperature
Reversible, observable microstructure

## Slide 4
How to probe a faster martensitic transformation?
Two important considerations:
High magnetic field pulse
THz pulse
Flash lamp pulse
Current pulse
Laser pulse
    How to induce a faster transformation?
    How to measure the faster transformation?
Direct delta T during transformation
Ultrafast electron microscopy
In-situ stress
Synchrotron diffraction
Phonon frequencies
MOKE

## Slide 5: Joule heating [1,2,3]
    How to probe the transformations?
[1] Vollach S. et. al., Scripta Mat. 2017;135:76-79.
[2] Aleksandr V. et al., Shap. Mem. Superelasticity 2018; 4:256–263
[3] Dana A. et. al. J. All. Comp. 2021;856:157968.
Joule heating:
heating by current pulse
M: martensite
A: austenite
1 µs
t [μs]
σ [MPa]
25 µs
Material: Ni-Ti wire
by pulsed current
by dynamic stress change during the transformation
Transformation from M → A within 25 µs

## Slide 6: Pulse laser heating [1]
    [1] S. Schwabe, S. Fähler* et al, Science and Technology of Advanced Materials 2022, Vol. 23, No. 1, 633–641
    How to probe the transformations?
by pulsed laser
by synchrotron diffraction during the martensitic transformation
Transform from M → A within 7 ns
Thin film transformation can be triggered within ~ns
Material: Ni-Mn-Ga 500 nm film
t (ns)
t = 7 ns
M
A
M

## Slide 7: Pulsed high magnetic field ‘cooling’[1]
    How to probe the transformations?
[1] Gottschall T. et. al. Phys Rev Appl. 2016;5:024013.
Material: Ni-Mn-In-Co bulk
Pulsed field: 10 T
Field duration: 10 ms
by pulsed magnetic field
by direct adiabatic temperature change during the transformation
Transformation from M → A is 13 ms.
Coupling crystal lattice and magnetic spins

## Slide 8: Why Ni-Mn-Ga based ferromagnetic film ?
[1] S. Schwabe, S. Fähler* et al. Adv. Funct. Mater. 2021, 31, 2005715
TB: Twin boundaries
    Question: are these levels obeyed or disturbed if in shorter time?
    Martensitic microstructure after a slower oven cooling[1]:
Microstructural level
Lattice level
    Multi-stages: able to realize multi-length scale observation

## Slide 9: PhD dissertation outline
    Ex-situ structural study
    Influence of flash lamp annealing (FLA) Paper planning
    Influence of pulsed high magnetic fields Experiments on-going
    In-situ study
    Direct delta T measurement during pulsed high magnetic fields
    Film patterning and thermocouple designing
    Synchrotron laser heating DESY 23.04-26.04.2023
    Joule heating Set-up construction

## Slide 10
Influence of flash lamp annealing on microstructures and transformations in ferromagnetic Ni-Mn-Ga epitaxial films
    Ex-situ study _ Project 1
Collaboration with FWIM @ HZDR:
Thomas Schumann
Dr. Lars Rebohle
Dr. Shengqiang Zhou

## Slide 11
[1] S. Schwabe, S. Fähler* et al. Adv. Funct. Mater. 2021, 31, 2005715
2D RSM: 2D Reciprocal Space Mapping
SEM: Scanning Electron Microscope
Microstructural level
Lattice level
Level 5: two martensitic variants
Type X and Type Y
(by SEM)
Level 1: two crystal structures
NM and 14M
(by 2D RSM and 2D Pole figure)
14M: orthorhombic 14-layer modulated martensite
NM: tetragonal nonmodulated martensite
    Characterization:
Twinning: {110} plane family

## Slide 12: Experiments:
What varied:
Flash energy density was adjusted from 14 ~ 83 J∙cm-2, respectively.
Notice: might some mismatch between calculated and experimental data
TM
Pulse : 3 ms
Simulated heating-cooling curve
Cooling rates
Heating temperatures
Heating rates
Flash Lamp Annealing (FLA)

## Slide 13
    As-deposited Ni-Mn-Ga:
Summarized from 2D RSM
≈ half : half
(by integration of peak area)
4µm
Substrate edges are parallel to the picture frame
Y
X
≈ half : half
(by MATLAB calculation)

## Slide 14
14M → NM: tetragonal distortion and thermally activated coarsening
Why 14M → NM?
The more stress, the more tetragonal distortion, the more stress goes to NM
The more energy, the more coarsening by annihilation of TBs, the smaller number of TBs and the enlarge of the TB-spacing, the more NM.
∑INM
∑I14M
After flash lamp annealing：
Summarized from 2D RSM

## Slide 15
Type Y
Type X
Why Type Y → Type X?
Based on Schmidt's law, Schmidt factor of Type Y = 0 but Schmidt factor of Type X = max. The more stress, the more Type X.
Different level of twin boundary motion
After flash lamp annealing：
Calculated by MATLAB
83 J∙cm-2
No FLA
55 J∙cm-2
10 µm
10 µm
10 µm
Y
X
X
Y
X

## Slide 16
Summary
Data not shown:
Pole figure measurements and calculations for orientations observations
Hysteresis loops and magnetic domain structures study
Regular wrinkles fast fast flash pulse, why and how?
Structural study of Ni-Mn-Ga film treated by faster flash pulse

## Slide 17
    Ex-situ study _ Project 2
Influence of high pulsed magnetic field on microstructures and transformations in ferromagnetic Ni-Mn-Ga-Cu epitaxial films
Collaboration with HLD @ HZDR:
Timo Niehoff
Dr. Tino Gottschall
Proposal Nr.: DMA13-222

## Slide 18
    As-deposited Ni-Mn-Ga-Cu:
Y
X
Type Y dominated film
In FLA section, TM = 650 K >> Tc = 320 K. M(T), M(H)…
So, in this HLD section, we use a modified Cu doped Ni-Mn-Ga film grown on STO (100).

## Slide 19
M(T) of Ni-Mn-Ca-Cu at 0.1T / 2T / 5T / 7T
Phase diagram [ TM v.s. H]
Heat the film above 370 K to get an austenite film by using an electric coil
Cool the film to 335 K which is at the hysteresis
At T = 335 K, probe the in-plane magnetic pulse going in the easy axis
After the pulse, cool the film to room temperature
Mf: martensite finish temperature
As: austenite start temperature
Ms: martensite start temperature
Af: austenite finish temperature
370K
335K
50 T, 1500 T s-1
300K
Experiments:

## Slide 20
After pulsed magnetic field (50 T, 1500T∙s-1):
before pulse
after pulse
Preliminary results shows that indeed something happened
Need more detailed check

## Slide 21
Next steps:
Summarize the characterization of the in-plane treatment
Do one more in-plane pulse but with 5 T.
Do out-of-plane pulse treatment

## Slide 22: Time-line
    Task of 2023
    Influence of Flash lamp annealing
    Paper submitted before 10.23
    Influence of pulsed high magnetic fields
    Experiments done and summarized before 12.23
    Direct delta T measurement with pulsed magnetic fields
    Experiments done before 12.23
    Synchrotron laser heating @ DESY 04.23 and summarized before 10.23
    Task of 2024
    Joule heating set-up testing and DESY
    Dissertation writing
    One paper is submitted to STAM on 02.23 Under reviewing

## Slide 23
Yuru Ge
Time dependency
Dr. Sebastian Fähler
Supervision
Lukas Fink
Thermomagnetic films
Dr. Klara Lünser
Epitaxial NiTi films
Bruno Neumann
Thermoelastic Harvesting
Satyakam Kar
Finite Size Effects
Dr. Lars Rebohle
FWIM
Thomas Schumann
FWIM
Dr. Shengqiang Zhou
FWIM
Mei Wu
FWIM
Timo Niehoff
HLD
Dr. Tino Gottschall
HLD
Dr. Fabian Ganss
FWIZ
Dr. René Hübner
FWIZ
Dr. Paul Chekhonin
FWOM
Thomas Naumann
FWIN
Prof. Peter Gaal
DESY
Mallika Khosla
DESY
Dr. Ciarán Fowley
FWIO
Prof. Gianaurelio Cuniberti
TU Dresden
Dr. Jürgen Lindner
FWIN
Dr. Kilian Lenz
FWIN
Fabian Samad
FWIN
Prof. Jürgen Faßbender
HZDR
Andreas Henschke
FWIN
Dr. Rysard Narkovic
FWIN

## Slide 25: Pulse laser heating [1]
    [1] S. Schwabe, S. Fähler* et al, Science and Technology of Advanced Materials 2022, Vol. 23, No. 1, 633–641
sample
Nanosecond Laser, repitition rate 1 kHz
Pulse duration
7 ns
Synchrotron radiation
(DESY Hamburg
Petra III P23)
100 ps
Delay generator
Triggers laser pulse
Triggers
detector measurement
Area detector
[2] Thanks to Dr. Klara Lünser for the sketch of the experimental set-up
Experimental set-up[2]
M
A
M
t (ns)
t = 16 ns
In-situ measuring by synchrotron x-ray diffraction, induced by pulsed laser, the martensitic transformation of Ni-Mn-Ga film from M → A within 16 ns
Material: Ni-Mn-Ga 500 nm film

## Slide 26
S. Kaufmann, et al, NJP 13, 053029 (2011)
14M is a nanotwinned adaptive phase, built from the NM unit cells, with the stacking periodicity (5)2 or (2)2.
14M: 14-layer modulated martensite
Stacking decribed from vertical direction ↑
(5)2
5 aNM
2 cNM
repeat 2 time
(2)2
2 aNM
5 cNM
repeat 2 time
= (5+2)*2 = 14-layer
NM unit cell
NM…? And, 14M → NM. Why ?

## Slide 27
[1] S. Kaufmann, et al., NJP 13, 053029 (2011)
[2] P. Entel, et al., J. Phys. D 39, 865 (2006)
14M: large amount of twin-boundary, exhibits higher energy, unfavourable and thermodynamically unstable [2], needs to energy-reducing.
How? Coarsening mechanism: by reducing twin-boundary numbers. ( (a)→(b) ). When reaches stable, we get NM. So, 14M → NM done.
The more heat driving, the heavy 14M → NM
Substrate
(a)
(b)
(c)
A unit cell
NM unit cell
14M → NM: thermally activated coarsening
14M[1]
NM
NM in macroscale

## Slide 28
(5)2
(2)2
Schwabe’s paper
Level 2
a/b-TBs
The red line

## Slide 29
Sketch of the continuum model
(Branching mechanism and Coarsening mechanism)
Substrate
A
M
Coarsening by annihilation of TBs, to reduce the number of TBs, then enlarge the TB-spacing
Branching of twin boundaries connecting to different variant orientations (blue and green)
TB-spacing
Branching connected the nanotwinned 14M (blue) and macroscopic NM (green), which slower the coarsening
Coarsening kill nano-TBs, which slower Branching
These two concept works together, to reach the final low-energy and harmonic state
K. Bhattacharya, Microstructure of Martensite, Oxford University Press, Oxford 2003.

## Slide 30
NM
2 5 2 5 …
Coarsening
Nanotwinned 14M

## Slide 31
50 T, 1500 T∙s-1